Effects of selected emulsion components; (bovine serum albumin, lipase and glutaraldehyde), on the surface properties of Polydimethylsiloxane.
by
Victoria Thobile Windvoel
Student no. 200806311

A dissertation submitted to the faculty of Science and Agriculture- Department of Biochemistry, at the University of Limpopo, Medunsa Campus, in fulfillment of the requirements for the degree of Masters of Science in Biochemistry.

January, 2011
DECLARATION
I declare that this dissertation is my own work. It is being submitted for the Degree of Master of Science in Biochemistry at the University of Limpopo, Medunsa Campus. This work has not been submitted for any other degree or examination in any other University. 

                               Victoria Thobile Windvoel



Day of 
year 

ABSTRACT
The purpose of this study was to investigate the effects of bovine serum albumin (BSA), lipase and glutaraldehyde on the surface of polydimethylsiloxane (PDMS). PDMS blocks of 15 by 15mm were fabricated using replica micromolding. To determine the effects of BSA, clean PDMS blocks were immersed in 20, 50 and 100mg/ml BSA, respectively. For the effect of lipase, the concentration was 20, 50 and 70mg/ml. To determine the effect of glutaraldehyde, 5, 10, 20, 30, 40 and 50% concentration was used. All the PDMS blocks were immersed for 10, 20 and 30 minutes. The water contact angle was measured on all the PDMS surfaces, including a clean surface as a control. This analysis was done using a drop shape analyzer, DSA 100 machine. The PDMS surfaces were further analyzed by Fourier Transform InfraRed (FTIR spectroscopy), using a Pelkin-Elmer FT-IR spectrometer. PDMS blocks which were pre-immersed in 5% glutaraldehyde and then in BSA and lipase solutions, respectively, were also added for FTIR analysis. The water surface tension was measured for both BSA and lipase and interfacial tension was measured for glutaraldehyde, using the DSA 100. The results indicated that the water contact angle decreases after the PDMS surface has been immersed in all the solutions prepared.  FTIR analysis showed new peaks on the PDMS surface immersed in BSA, and in BSA and glutaraldehyde; however, there were no peaks formed on the PDMS surface immersed in lipase and washed, in glutaraldehyde, and in lipase and glutaraldehyde together. Surface tension measurements showed that BSA and lipase decreases the surface tension of water. Interfacial tension measurements also showed that glutaraldehyde decreases the interfacial tension of oil. BSA, lipase and glutaraldehyde therefore decrease the hydrophobicity of the PDMS surface. BSA adsorbs on the PDMS surface and the adsorption is irreversible. The adsorption of lipase on the PDMS surface is reversible. Glutaraldehyde does not adsorb on the surface or the adsorption is not detectable. BSA, lipase and glutaraldehyde all have surface active properties. The CMC value of BSA is 50mg/ml and of lipase is 15mg/ml. 
Keywords: BSA, Glutaraldehyde, Lipase, Polydimethylsiloxane (PDMS)
DEDICATIONS

This work is dedicated to my unborn baby, for giving me a reason to work even harder and strive for success in everything I do. The love I have for you can never be put into words.

To my family and my baby-dad, thank you for the unconditional love, support and understanding, ALWAYS. God knows how grateful I am.

In loving memory of my mother! I know you are with me everywhere I go. May your soul forever rest in peace.
ACKNOWLEDGEMENTS
I would like to acknowledge the support which was provided by the Council for Scientific and Industrial Research, Mechatronics and Micromanufacturing. I came to CSIR with no clue what microfluidics was, but today I see it as a solution to many of the world’s problems. Thanks to the micromanufacturing team!
Special appreciation goes to the following people, for their assistance, constructive criticism and encouragement.

Dr M.A Mogale                                                                             (Supervisor)

Mr M. Mbanjwa and Mr K. Land                                                 (Co-Supevisors)
Miss L Kotze                                                                                (CSIR-P& C)

All members of the NSIA-MES project                                       (CSIR)

Last and certainly not least, all appreciation goes to the Almighty, for giving me the strength I needed to do this.

Thank you all!! 
TABLE OF CONTENTS                                                                PAGE
Declaration…………………………………………………………………………….II
Abstract………………………………………………………………………………III                                                                                                              
Dedications…………………………………………………………………………...IV
Acknowledgements…………………………………………………………………...V   
Table of contents……………………………………………………………………..VI                                                                      
List of figures………………………………………………………………………...IX
List of tables………………………………………………………………………....XI
List of non standard abbreviations…………………………………………………..XII
1. Background, problem statement and significance of study……………………1                                                                                                                     
1.1. Introduction of background…………………………………………………...1
1.2. Research problem statement………………………………………………….2     
1.3. Aim and objectives of study…………………………………………………..3
1.4. Significance of the study……………………………………………………...3
2. Literature review…………………………………………………………………4                                                                                
2.1 Introduction, aims and scope of the literature review…………………………4                                                                                       
2.2 Polydimethylsiloxane (PDMS) and its fabrication…………………………….4
2.2.1 Polydimethylsiloxane………………………………………………………..4
2.2.2 Fabrication of PDMS………………………………………………………..5                  
2.3 PDMS surface-protein interactions …………………………………………...6                                                                                      
2.4 Emulsion components for production of spherezymes………………………..7
2.4.1 Bovine serum albumin………………………………………………………7
2.4.2 Lipase………………………………………………………………………..7
2.4.3 Glutaraldehyde (a cross-linker)…………………………………………….. 8
2.4.4 Surfactants…………………………………………………………………...8
2.5 Analysis (measurement) of PDMS-surface interactions………………………9
2.5.1 Effects of surface active molecules on the hydrophobicity of PDMS………9
2.5.2 Wetting effects of a PDMS surface active substances……………………..10
2.5.3 Effects of surface active molecules on the chemical structure of PDMS….11
3. Materials and methods………………………………………………………….13
3.1 Materials……………………………………………………………………...13
3.1.1 Chemical reagents………………………………………………………….13                                                                                     
3.1.2 Apparatus and equipment…………………………………………………..13
3.2 Research design………………………………………………………………13                                                
3.3 Methods………………………………………………………………………14
3.3.1 Preparation (fabrication) of PDMS blocks…………………………………14
3.3.2 Effects of BSA on the PDMS surface……………………………………...14
3.3.2.1 Effect of the concentration of BSA on the PDMS surface……………….14
3.3.2.2 Effect of time of contact with BSA on the PDMS surface……………….14
3.3.3 Effects of lipase on the PDMS surface……………………………………..16
3.3.4 Effects of glut-EDA on the PDMS surface………………………………...16
3.3.5 Cross-linking effects of glutaraldehyde-EDA……………………………...17
3.3.5.1 BSA cross-linking effects………………………………………………...17
3.3.5.2 Lipase cross-linking effects………………………………………………17
3.3.6 Analysis of the PDMS surface effects of BSA, lipase and glutaraldehyde...17
3.3.6.1 Effects on the hydrophobicity of the PDMS surface…………………….17
3.3.6.2 Effects on the chemical structure of PDMS……………………………...18
3.3.6.3 Effects on the surface tension of water…………………………………..18
4. Results…………………………………………………………………………...19
4.1 Effects of BSA on the surface properties of PDMS………………………….19
4.1.1 Effects on hydrophobicity of the PDMS surface…………………………..19
4.1.2 Effects on the chemical structure of the PDMS surface……………………20
4.1.3 Effects on the surface tension of wate…………….......................................24
4.2 Effects of lipase on surface properties of PDMS…………………………….26
4.2.1 Effects on the hydrophobicity of the PDMS surface……………………….27
4.2.2 Effects on the chemical structure of the PDMS surface……………………31
4.2.3 Effetcs on the surface tension measurements………………………………32
4.2.4 Critical micelle concentration of lipase…………………………………….33
4.3 Effects of glutaraldehyde-EDA on the surface properties of PDMS………...33
4.3.1 Effects of glutaraldehyde-EDA on the hydrophobicity of PDMS…………33
4.3.2 Effects of glutaraldehyde-EDA on the chemical structure of PDMS……...34
4.3.3 Effects of glutaraldehyde-EDA on the interfacial tension…………………42
4.4 Cross-linking effects of glutaraldehyde-EDA………………………………..42
4.4.1 BSA cross-linking effects…………………………………………………..42

4.4.2 Lipase cross-linking effects………………………………………………...45
5. Discussions & Conclusions……………………………………………………..49
5.1 Effect of BSA on the surface properties of PDMS…………………………..49
5.2 Effect of lipase on the surface properties of PDMS………………………….50
5.3 Effect of glutaraldehyde-EDA on the surface properties of PDMS………….52
5.4 Cross-linking effects of glutaraldehyde-EDA………………………………..52
5.5 Limitations of the study………………………………………………………52
5.6 Conclusions and recommendations…………………………………………..52
6. References……………………………………………………………………….54
LIST OF FIGURES
Figure 1.1: Schematic representation of the spherezymes production…...……………1              
Figure 1.2: Polydispersity……………………………………….…………………….2
Figure 2.1: Repeating PDMS subunits…………………………….…………………..4                                                                                   
Figure 2.2: Fabrication of PDMS……………………………………….……………..5
Figure 2.3: Peroxide-based mechanism for cross-linking……………………………..6                                                       
Figure 2.4: Micellization phenomenon………………………………………………..9
Figure 2.5: Contact angle measurements……………………………………………...9
Figure 2.6: Using surface tension measurements to find the CMC…………………..11
Figure 2.7: Spectrum of a clean PDMS surface……………………………………...12
Figure 3.1: PDMS blocks immersed in BSA solutions………………………………15                                                  
Figure 3.2: Washing of PDMS blocks with PBS…………………………………….15
Figure 3.3: Drying of PDMS blocks inside an air chamber………………………….16                                      
Figure 3.4: FTIR spectra of a clean PDMS surface………………………………….18   
Figure 4.1: Droplets of water on BSA treated PDMS surface……………………….21
Figure 4.2: FTIR of 20mg/ml BSA treated PDMS surface…………………………..22                                                                                                                                                   
Figure 4.3: FTIR of 50mg/ml BSA treated PDMS surface…………………………..23                                    
Figure 4.4: FTIR of 100mg/ml BSA treated PDMS surface…………………………24                                   
Figure 4.5: Droplet of water during surface tension measurements………………….26  
Figure 4.6: Determination of the CMC value of BSA……………………………….27                               
Figure 4.7: Droplets of de-ionized water on lipase treated PDMS surfaces…………28
Figure 4.8: FTIR of 20mg/ml lipase treated PDMS surface…………………………29                                   
Figure 4.9: FTIR of 50mg/ml lipase treated PDMS surface…………………………30                                
Figure 4.10: FTIR of 70mg/ml lipase treated PDMS surface………………………..31
Figure 4.11: Droplets of water during surface tension measurements……………….33                                  
Figure 4.12: Determination of the CMC value of lipase……………………………..33                                                                                         
Figure 4.13: Droplets of de-ionized water on glut-EDA treated PDMS surface…….35                                           
Figure 4.14: FTIR of de-ionized water, EDA, glut and glut-EDA…………………...36                           
Figure 4.15: FTIR of 5% glutaraldehyde treated PDMS surface…………………….37                       
Figure 4.16: FTIR of 10% glutaraldehyde treated PDMS surface…………………...38                   
Figure 4.17: FTIR of 20% glutaraldehyde treated PDMS surface………………...…39
Figure 4.18: FTIR of 30% glutaraldehyde treated PDMS surface…………………...39
Figure 4.19: FTIR of 40% glutaraldehyde treated PDMS surface…………………...40                     
Figure 4.20: FTIR of 50% glutaraldehyde treated PDMS surface………………..….41                     

Figure 4.21: FTIR of 20mg/ml BSA-5% glut-EDA treated PDMS surface…………42
Figure 4.22: FTIR of 50mg/ml BSA-5% glut-EDA treated PDMS surface…………44
Figure 4.23: FTIR of 100mg/ml BSA-5% glut-EDA treated PDMS surface………..45
Figure 4.24: FTIR of 20mg/ml lipase-5% glut-EDA treated PDMS surface………...46
Figure 4.25: FTIR of 50mg/ml lipase-5% glut-EDA treated PDMS surface………...47
Figure 4.26: FTIR of 70mg/ml lipase-5% glut-EDA treated PDMS surface………...48
LIST OF TABLES
Table 3.1: Preparation of glut-EDA solutions………………………………………..16                                                                
Table 4.1: Average water contact angles of clean and BSA treated PDMS surfaces..20                                     
Table 4.2: Effects of BSA on the surface tension of water…………………………..25
Table 4.3: Average water contact angles of clean and lipase treated PDMS surfaces.27
Table 4.4: Effects of BSA on the surface tension of water…………………………..32
Table 4.5: Water contact angles of clean and glut-EDA treated PDMS surfaces……34
Table 4.6: Effect of glut-EDA on the interfacial tension of water…………………...43             
List of non standard abbreviations

ATR-FTIR- Attenuated total reflectance- Fourier transform infrared spectroscopy
BSA- Bovine serum albumin
CMC- Critical micelle concentration
EDA- Ethylene diamine
IFT- Interfacial tension
PBS- Phosphate buffer saline
PDMS- Polydimethylsiloxane
Si- Silicone
SiO2- Silicone dioxide
SPR- Surface plasminogen resonance
XPS- X-ray photoelectron spectroscopy
[image: image1.png]










































































































































































































































































































































I
9
XI

